

***NOVOPROOF***→ ***connection***

**paste PROPERTIES**: NOVOPROOFpaste→ connections permanently elastic, weather-resistant and is characterized by good adhesion to almost all common building surfaces, such as concrete, stone, wood, aluminum, steel, etc.

**POSSIBILITIES OF APPLICATION**: NOVOPROOFpaste→ Connections suitable for:

Permanently elastic sealing of connection joints, wall connection profiles and

sheet metal on roof structures of all kinds.

**storageSPECIFIC DATA:** Basis: Synthetic rubber

---------------------- -------------------------------------------------- ---

Color: black

-------------------------------------------- -------------------------------

Specific weight: approx. 1.23 g / cm³

------- -------------------------------------------------- ------------------

Shore A hardness: approx. 14

------------------------- --------------------------------------------------

Elongation at break: approx. 550%

-------------------------------------------- -------------------------------

Tensile strength: approx. 1.0 N / mm²

--------- -------------------------------------------------- ----------------

Processing: ≥ temperature+ 5 ° C

--------------------------- ------------------------------------------------

Storage: cool, dry and frost-free

--------------------------------------------- - ----------------------------- Storage

time: approx. 6 months

--------------- -------------------------------------------------- ----------

**SUBSTRATE CONSTRUCTION**: **PROCESSING**

The adhesive surfaces must be

dry, clean and free

of oils and greases.

**DELIVERY FORMCutthread neck**:cartridges á 310 ml

cartridge at the upper. Unscrew the spray nozzle and insert the cartridge into the hand gun.

The nozzle can be cut at an angle depending on the material requirements.

**HAZARD INFORMATION Avoid**:contact with skin and eyes. Keep out of the reach of children. During the hardening process (approx. 1 week) small amounts of harmful

substances are released, so it is essential to ensure good ventilation during this time.

**If our processing instructions are not observed, the risk of damage to health cannot be ruled out.**

**DURAPROOF** technologies GmbH, Eisenbahnstrasse 24, 66687 Wadern-Büschfeld